Samurai DPSS laser

Utah Nanofab Development

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| **Material** | **Notes** | **Power (%)** | **Passes (#)** | **Speed (mm/s)** | **Freq (kHz)** |  |
| PEI film | McMaster 7576K23  .01” thick | 100 | 100 | 500 | 30 |  |
| 260 Brass | McMaster 9011K201  0.002” thick | 100 | 15 | 100 | 30 | Profile “DRL Brass Shim” |
|  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |