TMV Characterization Procedure

Using silicon oxide wafers

- Use zygo profilometer to test for surface roughness.

- Use four-point probe to test for surface conductivity in 5 different places on the wafer.  Top, middle, bottom, left, right.

- Run test wafer through Tencor FLX 2320 thin film stress measurement device.

- Run test wafer through TMV sputtering system.

- Rerun test wafer through Tencor FLX 2320 thin film measurement device.

- Go grab a sandwich.

- Use zygo profilometer to test for surface roughness.

- Use four-point probe to test for surface conductivity in 5 different places on the wafer.  Top, middle, bottom, left, right.

- Etch wafer and test for film thickness and uniformity in 5 different places on the wafer.  Top, middle, bottom, left, right.

- Enter data into spreadsheet and publish to web page.

- Use nanospec to measure film thickness